DATA SHEET

SURFACE-MOUNT CERAMIC MULTILAYER CAPACITORS

Class 2, Y5V

16/25/50 V

Preliminary specification – Dec 26, 2005 V.11

| Phycomp | Product specification |
| --- | --- |
| Surface-mount ceramic | Class 2, Y5V |
| multilayer capacitors | 16/25/50 V |

FEATURES

- Five standard sizes

- High capacitance per unit volume

- Supplied in tape on reel

- NiSn terminations.

APPLICATIONS

- Consumer electronics, for example:

−  Tuners

− Television receivers − Video recorders

− All types of cameras − Mobile telephones.

DESCRIPTION

The capacitor consists of a rectangular block of ceramic dielectric in which a number of interleaved metal electrodes are contained. This structure gives rise to a high capacitance per unit volume.

The inner electrodes are connected to the two terminations and finally covered with a layer of plated tin (NiSn). A cross section of the structure is shown in Fig.1.

QUICK REFERENCE DATA

| DESCRIPTION | VALUE |
| --- | --- |
| Rated voltage UR (DC) | 16 V, 25 V, 50 V |
| Capacitance range (E6 series) | 10 nF to 10 µF; note 1 |
| Tolerance on capacitance | 20% (M); −20% to 80% (Z) |
| Test voltage (DC) for 1 minute: | 2.5  UR |
| Sectional specifications | IEC 60384-10, second edition 1989-04 |
| Detailed specification | based on IEC 60384-10-1 |
| End terminations | NiSn |
| Climatic category (IEC 60068) | 30/85/21 |

Note

1.	Measured at 25 C, 1 V and 1 kHz, using a four-gauge method.

terminations

electrodes

MLB457

ceramic material

Fig.1	Construction of a ceramic multilayer capacitor.

2005 Dec 26 Rev.11	2	www.yageo.com

Phycomp	Product specification

| Surface-mount ceramic | Class 2, Y5V |
| --- | --- |
| multilayer capacitors | 16/25/50 V |
| MECHANICAL DATA |  |

T	W

L2  L4   L3

L1	MBB211

For dimensions see Table 1.

|  |  |  |  | Fig.2. |  | Component outline. |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Physical dimensions |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Table 1 Capacitor dimensions; see Fig.2 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| CASE SIZE | L1 |  | W |  |  |  | T |  |  | L2 and L3 . |  | L4 |  |
|  |  |  |  |  |  | MIN. |  | MAX. | MIN. |  | MAX. | MIN. |  |
| Dimensions in millimetres |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 0402 | 1.0 0.05 | 0.5 0.05 |  |  |  | 0.45 |  | 0.55 | 0.15 |  | 0.30 | 0.40 |  |
| 0603 | 1.6 0.10 | 0.8 0.07 |  |  |  | 0.73 |  | 0.87 | 0.25 |  | 0.65 | 0.40 |  |
| 0805 | 2.0 0.10 | 1.25 |  | 0.10 |  | 0.50 |  | 1.35 | 0.25 |  | 0.75 | 0.55 |  |
| 1206 | 3.2 0.15 | 1.6 0.15 |  |  |  | 0.50 |  | 1.75 | 0.25 |  | 0.75 | 1.40 |  |
| 1210 | 3.2 0.20 | 2.5 0.20 |  |  |  | 1.40 |  | 1.60 | 0.25 |  | 0.75 | 1.40 |  |
| Dimensions in inches |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 0402 | 0.040 0.002 | 0.020 |  | 0.002 |  | 0.018 |  | 0.022 | 0.008 |  | 0.012 | 0.016 |  |
| 0603 | 0.063 0.004 | 0.032 |  | 0.003 |  | 0.029 |  | 0.035 | 0.010 |  | 0.026 | 0.016 |  |
| 0805 | 0.079 0.004 | 0.049 |  | 0.004 |  | 0.020 |  | 0.053 | 0.010 |  | 0.030 | 0.022 |  |
| 1206 | 0.126 0.006 | 0.063 |  | 0.006 |  | 0.020 |  | 0.069 | 0.010 |  | 0.030 | 0.056 |  |
| 1210 | 0.126 0.008 | 0.098 |  | 0.008 |  | 0.047 |  | 0.069 | 0.010 |  | 0.030 | 0.056 |  |

2005 Dec 26 Rev.11	3	www.yageo.com

Phycomp	Product specification

| Surface-mount ceramic |  |  |  |  |  |  |  |  |  | Class 2, Y5V |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| multilayer capacitors |  |  |  |  |  |  |  |  |  | 16/25/50 V |  |  |  |
| SELECTION CHART FOR 16 V AND 25 V |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | LAST |  |  |  | 16 V |  |  |  | 25 V |  |  |  |  |
| C | TWO |  |  |  |  |  |  |  |  |  |  |  |  |
|  | DIGITS |  |  |  |  |  |  |  |  |  |  |  |  |
| (nF) |  | 0402 | 0603 |  | 0805 | 1206 | 1210 | 0603 | 0805 | 1206 | 1210 |  |  |
|  | OF |  |  |  |  |  |  |  |  |  |  |  |  |
|  | 12NC |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | 23 |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.5 | 25 |  |  |  |  |  |  |  |  |  |  |  |  |
| 2.2 | 27 |  |  |  |  |  |  |  |  |  |  |  |  |
| 3.3 | 29 |  |  |  |  |  |  |  |  |  |  |  |  |
| 4.7 | 32 |  |  |  |  |  |  |  |  |  |  |  |  |
| 6.8 | 34 |  |  |  |  |  |  |  |  |  |  |  |  |
| 10 | 36 | 0.5 0.05 |  |  |  |  |  | 0.8 0.07 |  |  |  |  |  |
| 15 | 38 |  |  |  |  |  |  |  |  |  |  |  |  |
| 22 | 41 |  |  |  |  |  |  |  |  |  |  |  |  |
| 33 | 43 |  |  |  |  |  |  |  |  |  |  |  |  |
| 47 | 45 |  |  |  |  |  |  |  |  |  |  |  |  |
| 68 | 47 |  |  |  |  |  |  |  |  |  |  |  |  |
| 100 | 49 |  |  |  |  |  |  |  | 0.6 0.1 | 0.6 0.1 |  |  |  |
| 150 | 52 |  | 0.8 0.07 |  |  |  |  |  | 0.85 0.1 |  |  |  |  |
| 220 | 54 |  |  |  |  |  |  |  |  |  |  |  |  |
| 330 | 56 |  |  |  |  |  |  |  |  |  |  |  |  |
| 470 | 58 |  |  |  | 0.85 0.1 |  |  |  |  | 0.85 0.1 |  |  |  |
| 680 | 61 |  |  |  |  |  |  |  |  |  |  |  |  |
| 1,000 | 63 |  |  |  |  | 0.85 0.1 |  |  |  | 1.15 0.1 |  |  |  |
| 2,200 | 67 |  |  |  |  | 1.15 0.1 |  |  |  | 0.85 0.1 |  |  |  |
| 4,700 | 72 |  |  |  |  | 0.85 0.1 |  |  |  | 0.85 0.1 |  |  |  |
| 10,000 | 76 |  |  |  |  | 1.15 0.1 | 1.5 0.1 |  |  | 1.15 0.1 | 1.5 0.1 |  |  |

Note

1. Values in shaded cells indicate thickness class in mm.

2005 Dec 26 Rev.11	4	www.yageo.com

Phycomp	Product specification

| Surface-mount ceramic |  |  |  |  |  | Class 2, Y5V |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| multilayer capacitors |  |  |  |  |  | 16/25/50 V |  |  |
| SELECTION CHART FOR 50 V |  |  |  |  |  |  |  |  |
|  | LAST |  |  | 50 V |  |  |  |  |
| C | TWO |  |  |  |  |  |  |  |
|  | DIGITS |  |  |  |  |  |  |  |
| (nF) |  | 0603 |  | 0805 |  | 1206 |  |  |
|  | OF |  |  |  |  |  |  |  |
|  | 12NC |  |  |  |  |  |  |  |
| 10 | 05 | 0.8 0.07 |  | 0.6 0.1 |  |  |  |  |
| 15 | 06 |  |  |  |  |  |  |  |
| 22 | 07 |  |  |  |  |  |  |  |
| 33 | 08 |  |  |  |  |  |  |  |
| 47 | 09 |  |  |  |  |  |  |  |
| 68 | 11 |  |  |  |  |  |  |  |
| 100 | 12 |  |  |  |  | 0.6 0.1 |  |  |
| 150 | 13 |  |  | 0.85 0.1 |  |  |  |  |
| 220 | 14 |  |  |  |  |  |  |  |
| 330 | 15 |  |  |  |  |  |  |  |
| 470 | 16 |  |  |  |  | 0.85 0.1 |  |  |
| 680 | 17 |  |  |  |  |  |  |  |
| 1 000 | 18 |  |  |  |  | 1.15 0.1 |  |  |

Note

1. Values in shaded cells indicate thickness class in mm.

Thickness classification and packing quantities

|  | THICKNESS |  | 8 mm TAPE WIDTH QUANTITY PER REEL |  |  |  | QUANTITY PER BULK CASE |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | CLASSIFICATION |  | 180 mm; 7" |  | 330 mm; 13" |  | 0402 | 0603 | 0805 |  |
|  | (mm) |  |  |  |  |  |  |  |  |  |
|  |  |  | PAPER | BLISTER | PAPER | BLISTER |  |  |  |  |
|  | 0.5 0.05 |  | 10 000 | − | 50 000 | − | 50 000 | − | − |  |
|  | 0.6 0.10 |  | 4 000 | − | 20 000 | − | − | − | 10 000 |  |
|  | 0.8 0.07 |  | 4 000 | − | 15 000 | − | − | 15 000 | − |  |
|  | 0.85 0.10 |  | 4 000 | − | 15 000 | − | − | 15 000 | 8 000 |  |
|  | 1.15 0.10 |  | − | 3 000 | − | 10 000 | − | − | − |  |
|  | 1.25 0.10 |  | − | 3 000 | − | 1 000 | − | − | 5 000 |  |
|  | 1.5 0.10 |  | − | 3 000 | − | − | − | − | − |  |

2005 Dec 26 Rev.11	5	www.yageo.com

| Phycomp | Product specification |
| --- | --- |
| Surface-mount ceramic | Class 2, Y5V |
| multilayer capacitors | 16/25/50 V |

ORDERING INFORMATION

Components may be ordered by using either a Phycomp’s unique 12NC or simple 15-digit clear text code.

Ordering code 12NC (preferred)

handbook, full pagewidth

2 2 X X	X X X	X 9 X X X

| Carrier type |  | Capacitance value(1) |
| --- | --- | --- |
| 22 | blister |  |
| 38 | paper |  |
| 54 | bulk |  |

| Rated voltage - Termination |  |  | Tolerance |  |  |
| --- | --- | --- | --- | --- | --- |
| 78 | 16 V; NiSn |  | 7 | 20% |  |
| 91 | 25 V; NiSn |  | 8 | −20/80% |  |
| 58 | 50 V; NiSn |  |  |  |  |
| Size |  |  |  |  |  |
| 7 | 0402 |  | Packaging(2) |  |  |
| 6 | 0603 |  |  |  |  |
| 0 | 0805 |  | 1 | reel: 180 mm; 7" |  |
| 1 | 1206 |  | 5 | reel: 330 mm; 13" |  |
| 2 | 1210 | CCA620_a | 4 | bulk case |  |

- Refer to chapters “Selection chart for 16 V and 25 V” and “Selection chart for 50 V”.

- Quantity on reel depends on thickness classification, see section “Thickness classification and packing quantities”.

Phycomp Clear text code

EXAMPLE: 12062F105M8BB0D

| Size | Temp. | Capacitance |  | Tol. | Vol. | Termination | Packing | Marking | Series |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Code | Char. |  |  |  |  |  |  |  |  |  |
| 0402 | 2F = Y5V | 105 = 1000000 |  | M = 20% | 7 = 16 V | B = NiSn | 2 = 180 mm; 7" paper | 0 = no marking | D = BME |  |
| 0603 |  | pF; the third digit |  | Z = −20% /80% | 8 = 25 V |  | 3 = 330 mm; 13" paper |  |  |  |
| 0805 |  | signifies the |  |  | 9 = 50 V |  | B = 180 mm; 7" blister |  |  |  |
|  |  | multiplying factor: |  |  |  |  | F = 330 mm; 13" blister |  |  |  |
| 1206 |  |  |  |  |  |  |  |  |  |  |
|  |  | 2 | = × 100 |  |  |  | P = bulk case |  |  |  |
| 1210 |  |  |  |  |  |  |  |  |  |  |
|  |  | 3 | = × 1000 |  |  |  |  |  |  |  |
|  |  | 4 | = × 10 000 |  |  |  |  |  |  |  |
|  |  | 5 | = × 100 000 |  |  |  |  |  |  |  |
|  |  | 6 | = × 1 000 000 |  |  |  |  |  |  |  |

2005 Dec 26 Rev.11	6	www.yageo.com

| Phycomp | Product specification |
| --- | --- |
| Surface-mount ceramic | Class 2, Y5V |
| multilayer capacitors | 16/25/50 V |

ELECTRICAL CHARACTERISTICS

Class 2 capacitors; Y5V dielectric; NiSn terminations

Unless otherwise stated all electrical values apply at an ambient temperature of 25 1 C, an atmospheric pressure of 86 to 105 kPa, and a relative humidity of 63 to 67%.

| DESCRIPTION | VALUE |  |
| --- | --- | --- |
| Capacitance range (E6 series); note 1 | 10 nF to 10 µF |  |
| Tolerance on capacitance after 1000 hours | 20% (M); −20% to 80% (Z) |  |
| Tan δ; note 1: |  |  |
| all 25 V and 50 V |  |  |
| except 0805 ≥ 330 nF; 0603 /100 nF; 1206 /1 µF; 1210 /10 µF | ≤5% |  |
| sizes 0805 / 330 nF; 0603 / 100 nF; 1206 /1 F | ≤7% |  |
| 25 V |  |  |
| 0805 ≥ 470 nF | ≤9% |  |
| 1210 /10 µF | ≤12.5% |  |
| all 16 V |  |  |
| except 0402; 0603 ≥ 330 nF; 0805 ≥ 1.5 F; 1206 ≥ 3.3 F; 1210 /10 F | ≤9% |  |
| sizes 0402; 0603 ≥ 330 nF; 0805 ≥ 1.5 F; 1206 ≥ 3.3 F; 1210 /10 F | ≤12.5% |  |
| Insulation resistance after 1 minute at UR (DC): | Rins 10 GΩ or Rins  C ≥500 seconds |  |
|  | whichever is less |  |
| Maximum capacitance change with respect to capacitance at 25 °C | 22% to −82% |  |
| (for typical values see Fig.5) |  |  |
| Ageing | typical 7% per time decade |  |
| Resistance to soldering heat | 260 °C; 10 seconds |  |

Note

- Measured at 25 C, 1 V, 1 kHz, using a four-gauge method.

2005 Dec 26 Rev.11	7	www.yageo.com

| Phycomp | Product specification |
| --- | --- |
| Surface-mount ceramic | Class 2, Y5V |
| multilayer capacitors | 16/25/50 V |

MBD076

∆ C	0

C

(%)

20

40

60

80

100

| 0 | 10 | 20 | 30 | 40 | 50 |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | VDC (V) |  |

Fig.3	Typical capacitance change with respect to the capacitance at 1 V as a function of DC voltage at 25 C.

MBD077

25

∆ C C

(%)

0

25

50

75

100

25	0 25 50 75 100 T (oC)

MBD078

2000

tan δ

(x 10	4 )

1500

1000

500

0

25	0 25 50 75 100 T (oC)

Fig.4	Typical tan δ as a function of temperature.

Fig.5	Typical capacitance change

as a function of temperature.

2005 Dec 26 Rev.11	8	www.yageo.com

Phycomp	Product specification

| Surface-mount ceramic |  |  |  | Class 2, Y5V |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| multilayer capacitors |  |  |  | 16/25/50 V |  |  |
| TESTS AND REQUIREMENTS |  |  |  |  |  |  |
| Table 2 Test procedures and requirements |  |  |  |  |  |  |
| IEC | IEC |  |  |  |  |  |
| 60384-10/ | 60068-2 | TEST | PROCEDURE | REQUIREMENTS |  |  |
| CECC 32 100 | TEST |  |  |  |  |  |
| CLAUSE | METHOD |  |  |  |  |  |
| 4.4 |  | mounting | the capacitors may be mounted | no visible damage |  |  |
|  |  |  | on printed-circuit boards or |  |  |  |
|  |  |  | ceramic substrates by applying |  |  |  |
|  |  |  | wave soldering, reflow soldering |  |  |  |
|  |  |  | (including vapour phase |  |  |  |
|  |  |  | soldering) or conductive |  |  |  |
|  |  |  | adhesive |  |  |  |
| 4.5 |  | visual inspection and | any applicable method using 10 | in accordance with |  |  |
|  |  | dimension check | magnification | specification |  |  |
| 4.6.1 |  | capacitance | f = 1 kHz; Y5V measuring | within specified tolerance |  |  |
|  |  |  | voltage 1 Vrms at 25 C |  |  |  |
| 4.6.2 |  | tan δ | f = 1 kHz; Y5V measuring | in accordance with |  |  |
|  |  |  | voltage 1 Vrms at 25 C | specification |  |  |
| 4.6.3 |  | insulation resistance | at UR (DC) for 1 minute | RiCR ≥500 s |  |  |
| 4.6.4 |  | voltage proof | 2.5  UR for 1 minute | no breakdown or flashover |  |  |
| 4.7.1 |  | temperature | between minimum and maximum | in accordance with |  |  |
|  |  | coefficient | temperature | specification |  |  |
| 4.8 |  | adhesion | a force of 5 N applied for 10 s to | no visible damage |  |  |
|  |  |  | the line joining the terminations |  |  |  |
|  |  |  | and in a plane parallel to the |  |  |  |
|  |  |  | substrate |  |  |  |
| 4.9 |  | bond strength of | mounted in accordance with IEC | no visible damage |  |  |
|  |  | plating on end face | 60384-1, paragraph 4.35 |  |  |  |
|  |  |  | conditions: | ∆C/C: ≤30% |  |  |
|  |  |  | bending 1 mm at a rate of 1 |  |  |  |
|  |  |  | mm/s, radius jig 340 mm |  |  |  |
| 4.10 | Tb | resistance to | preconditioning: | the terminations shall be |  |  |
|  |  | soldering heat | 120 to 150 °C during 1 minute; | well tinned |  |  |
|  |  |  |  | after recovery ∆C/C: 20% |  |  |
|  |  |  | 260 5 °C for 10 0.5 s in a |  |  |  |
|  |  |  | static solder bath | tan δ: original specification |  |  |
|  |  |  |  | Rins: original specification |  |  |
|  |  | resistance to | 260 5 C for 30 1 s | using visual enlargement |  |  |
|  |  | leaching | in a static solder bath | of 10, dissolution of the |  |  |
|  |  |  |  | terminations shall not |  |  |
|  |  |  |  | exceed 10% |  |  |

2005 Dec 26 Rev.11	9	www.yageo.com

Phycomp	Product specification

| Surface-mount ceramic |  |  |  | Class 2, Y5V |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| multilayer capacitors |  |  |  | 16/25/50 V |  |  |
| IEC | IEC |  |  |  |  |  |
| 60384-10/ | 60068-2 | TEST | PROCEDURE | REQUIREMENTS |  |  |
| CECC 32 100 | TEST |  |  |  |  |  |
| CLAUSE | METHOD |  |  |  |  |  |
| 4.11 | Ta | solderability | zero hour test, and test after | the terminations shall be |  |  |
|  |  |  | storage (20 to 24 months) in | well tinned |  |  |
|  |  |  | original packing in normal |  |  |  |
|  |  |  | atmosphere; |  |  |  |
|  |  |  | unmounted chips completely |  |  |  |
|  |  |  | immersed for 2 0.5 s in a |  |  |  |
|  |  |  | solder bath at 235 5 C |  |  |  |
| 4.12 | Na | rapid change of | preconditioning: | no visible damage |  |  |
|  |  | temperature | between minimum and | after 48 hours recovery: |  |  |
|  |  |  | maximum temperature, 5 cycles | C/C: ≤ 20% |  |  |
| 4.14 | Ca | damp heat, | initialization: | no visible damage |  |  |
|  |  | steady state | 48 4 hours after UR at 40 °C | after 48 hours recovery: |  |  |
|  |  |  | for 1 hour (for initial value | C/C: 30%/−40% |  |  |
|  |  |  | measurement); | tan δ: ≤15% |  |  |
|  |  |  | 500 12 hours at 40 °C; | Rins: 500 MΩ or RiCR ≥ 100 s, |  |  |
|  |  |  | 90 to 95% RH; UR applied | whichever is less |  |  |
|  |  | damp heat; | initialization: | preconditioning: |  |  |
|  |  | with UR load | 48 hours after UR at 40 °C; | UR at 40 C for 1 hour, after |  |  |
|  |  |  | for 1 hour (for initial value | 48 hours recovery: |  |  |
|  |  |  | measurement); |  |  |  |
|  |  |  |  | C/C: 30%/−40% |  |  |
|  |  |  | 500 12 hours at 40 °C; |  |  |  |
|  |  |  |  | tan δ: ≤15% |  |  |
|  |  |  | 90 to 95% RH; UR applied |  |  |  |
|  |  |  |  | Rins: 500 MΩ or RiCR ≥ 25 s, |  |  |
|  |  |  |  | whichever is less |  |  |
| 4.15 |  | endurance | initialization: | after 48 hours recovery: |  |  |
|  |  |  | 2  UR at 85 C for 1 hour, | C/C: 30%/−40% |  |  |
|  |  |  | (initial value measurement after | tan δ: ≤15% |  |  |
|  |  |  | 48 4 hours) ; | Rins: 1000 MΩ or RiCR ≥ 50 s, |  |  |
|  |  |  | 2  UR at 85 C for 1000 hours | whichever is less |  |  |
|  |  |  | recovery 48 4 hours at room |  |  |  |
|  |  |  | temperature |  |  |  |

2005 Dec 26 Rev.11	10	www.yageo.com

Phycomp	Product specification

| Surface-mount ceramic |  |  | Class 2, Y5V |  |  |
| --- | --- | --- | --- | --- | --- |
| multilayer capacitors |  |  | 16/25/50 V |  |  |
| REVISION HISTORY |  |  |  |  |  |
| Revision | Date | Change | Description |  |  |
|  |  | Notification |  |  |  |
| Rev.11 | Dec 26, 2005 |  | Revised thickness of Y5V 0805 25/50 V 0.33 µF |  |  |
| Rev 10 | Sep 21, 2005 | − | Y5V 0805 16 V thickness revised and range extended from 2.2 |  |  |
|  |  |  | µF to 4.7 µF |  |  |
| Rev.9 | June 24, 2005 | − | - Revised thickness of: |  |  |
|  |  |  | Y5V 1206 16 V from 4.7 µF to10 µF |  |  |
|  |  |  | Y5V1206 25 V from 2.2 µF to 10 µF |  |  |
| Rev.8 | Jan 13, 2005 | − | - Revised thickness of Y5V 0805 16 V 1 µF and Y5V 0805 25 V 470 |  |  |
|  |  |  | nF to 1 µF |  |  |
| Rev.7 | Jul 08, 2003 | − | - Updated company logo |  |  |

2005 Dec 26 Rev.11	11	www.yageo.com